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1 3/4" (45mm) Round Radial Patch
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  Always wear safety goggles to protect your eyes, and wear other appropriate safety items for protection.  

Product Description


1 3/4" (45mm) Round Radial Patch; Thick Rubber Reinforced radial patch is one of the finest tire patches made today. BlackJack radial patches are thick, rubber-reinforced patches which allow placement on the tire in any direction. This repair can also be used on bias-ply tires. These patches work best when used with any of our string repair units. These patches are of a 2 piece construction made of virgin rubber on a bed of black cushion gum.

Usage Instructions


1. Inflate the tire to normal operating pressure to find the leak. A leak in the tire can be located by dipping the tire in a water bath or by spraying it with a leak detector such as BJ245. BlackJack leak detector is easy to use and can be used anywhere. It can locate even smaller leaks in the tread or around the tire bead and it is less bulky than a water bath.

2. Mark the injury with a tire-marking paint stick (BJPMW, BJPY, BJPW).

3. Mark the position of any wheel weights to be replaced after the tire is remounted on the wheel.

4. Remove puncture-causing foreign object(s) from the tire.

5. Inspect the injury to check for structural damage.

6. Swab the beads of tire using BJ44 Glide Tire Bead Lubricant for easy dismounting of the tire.

7. Remove the tire from the wheel and place on a tire spreader. Do not invert a radial tire. Thoroughly inspect the inside of the tire for additional damage.

8. Mark the inside of the tire where penetrating object entered the inner butyl liner.

9. Clean the area with BJ125 Rubber Buffer/Cleaner and scrape inner lining of tire with tire scraper BJ92 to remove silicone and mold release. NOTE: It is very important to remove this mold release before it is mechanically buffed.

10. Inside the marked area, mechanically buff interior rubber surface of tire to smooth velvet black. Be careful not to buff through the inner liner.

11. Vacuum or wipe-off excess buffing dust.

12. Apply a thin coat of BlackJack Tire Repair Cement to the cleaned/buffed area. Allow cement to dry completely (this may take longer on cool or humid days). NOTE: Do not burn off cement.

13. Remove backing from the reinforced boot patch (do not touch back of patch). Center patch over injury making sure bead arrows are pointing toward the beads and stitch down thoroughly.

14. Stitch patch down firmly with BJ99 Ball Bearing Stitcher. Start from center of the patch working outward in both directions. After stitching is complete, remove top cover film from patch. (On a tubeless tire, fill the injury with BlackJack Tire Repair BJ460 or BJ945 to prevent moisture from penetrating the tire.)

15. Apply BJ528 Butyl liner repair to seal over the finished repair and repair the butyl rubber liner where the tire where buffed.

16. Check the beads and rim for rust and damage. If there is damage to the bead or rust on the rim, coat the bead and/or rim with bead seal BJ228.

17. Remount and inflate the tire to its proper operating pressure.

18. Check for any additional leaks.

